## Slide 1
Imaging nano particles during crystal growth using atomic force microscopy
Christine V. Putnis
Institut für Mineralogie, University of Münster, Germany
Department of Chemistry, Curtin University, Perth, Australia
putnisc@uni-muenster.de; christine.putnis@curtin.edu.au
Notes: 1

## Slide 2
The nano world:
Nano-particles are all around us. The world is made up from nano-particles.
Advanced analytical techniques have enabled us to image was was previously only postulated.
What is more, they are worth billions of dollars – we pay billions to make them and billions to get rid of them!
Notes: 2

## Slide 3
cantilever
O-ring
sample
scanner
cup mount
fluid in
fluid out
Diagrams: JM Astilleros
AFM Nanoscale observations

## Slide 4
Desorción libre de agua
Bruker MultiMode AFM in Münster

## Slide 5
Bruker Fastscan AFM
in Curtin University, Perth

## Slide 7
Morphology of dissolution features of calcite
Notes: 7

## Slide 8
D
Dissolution rates of calcite in the presence of various ions
Etch pit spreading rates (open symbols) vs. dissolution rates (filled symbols)
IS = 0.001 M
(b) IS = 0.1M for the different
electrolytes tested.
Notes: 8

## Slide 9
Nanoscale observations – calcite growth
Growth mechanisms on calcite {10-14} surfaces as seen by AFM:
(a) spiral growth;
(b) two-dimensional nucleation or island growth.
Notes: 9

## Slide 10
Nanoscale observations – calcite growth
Development of reverse morphologies in spiral hillocks: (a) growth hillock formed during growth in NaCl-bearing solutions;
(b) the same spiral in (a) after changing the background electrolyte of the growth solution to CsCl.
Images are 10 mm x 10 mm.
Notes: 10

## Slide 11
Nanoscale observations – calcite growth and dissolution
Changes in the morphology of (a,b,d,e) growth and (c,f) dissolution features induced by the presence of additives. (a,b) Growth spirals; and (c) etch pits formed in pure solutions. The same features in (a,b,c) after adding (d) L-aspartic acid;
(e,f) Li+ to the solution.
Notes: 11

## Slide 12
Nanoscale observations – calcite growth in the presence of Se
1 μm
Notes: 12

## Slide 13
Nanoscale observations – calcite growth in the presence of Se
1 μm
Notes: 13

## Slide 14
Nanoscale observations – calcite growth in the presence of Se
1 μm
Notes: 14

## Slide 15
Nanoscale observations – calcite growth in the presence of Se
1 μm
Notes: 15

## Slide 16
Nanoscale observations – calcite growth in the presence of Se
1 μm
Notes: 16

## Slide 17
Nanoscale observations – calcite growth in the presence of Se
1 μm
Notes: 17

## Slide 18
Nanoscale observations – calcite growth in the presence of Se
Notes: 18

## Slide 19
Crystal growth from undersaturated solutions?
Nanoscale observations
Notes: 19

## Slide 20
Supersaturation of an aqueous solution relative to a simple stoichiometric end-member solid.
The thermodynamic definition of supersaturation :
Ω =
IAP
Ksp
For a simple mineral such as calcite CaCO3, for example
Ω =
{Ca2+}.{CO32-}
Ksp

## Slide 21
Calcite dissolving in the presence of 50 mM solution of (NH4)2HPO4
Surface 5x5 µm
T 2.5 h
Notes: 21

## Slide 22
Calcite dissolving in the presence of 50 mM solution of (NH4)2HPO4
1 mm
Notes: 22

## Slide 23
Dissolution of Cararra marble (CaCO3) in the presence of (NH4)2HPO4
unreacted
2 days 200°C
4 days 200°C
6 days
200°C
Images:
E. Trindade Pedrosa
Notes: 23

## Slide 24
Notes: 24

## Slide 25
Notes: 25

## Slide 26
Notes: 26

## Slide 27
Notes: 27

## Slide 28
Notes: 28

## Slide 29
Notes: 29

## Slide 30
The mineral-surface assisted formation of Ca-P phases may proceed through the aggregation of metastable clusters, rather than by addition of ions or molecules to a nucleus, and subsequently form stable ACP plates prior to the transformation to the final crystalline phase.
Posner’s clusters (Posner and Betts, 1975)
Notes: 30

## Slide 31
Calcite dissolving in the presence of Se ions

## Slide 32
Notes: 32

## Slide 33
Brucite Mg(OH)2 dissolution
Direct in situ observations of brucite dissolution in water in contact CO2 pH 3.5

## Slide 34
Notes: 34

## Slide 35
Morphology of dissolution features of brucite

## Slide 36
Dissolution - Precipitation

## Slide 37
Dissolution - precipitation
Dissolution of brucite and precipitation of Mg-carbonate

## Slide 38
Notes: 38

## Slide 39
Notes: 39

## Slide 40
Notes: 40

## Slide 41
In situ AFM observations of dolomite Ca,Mg(CO3)2 dissolution (pH 7)
d
e
t = 1312´
t = 1142´
a
b
t = 0´
t = 313´
c
t = 699´
f
t = 1569´
Notes: However, from our in situ, nanoscale observations of the reacting surface we found no experimental evidence that supports the hypothesis of a preferential release of calcium. Moreover, our AFM results clearly indicate that this “incongruent” behavior (non-stoichiometric dissolution) is the result of a dissolution-precipitation process. According to our observations, dolomite dissolution occurs at step edges parallel to < 41>, and dissolution at such step edges is a stoichiometric process, i.e. equal amounts of Ca2+ and Mg2+ are present along such steps and thus are equally released to the solution as the steps spread.

## Slide 42
In situ AFM observations of dolomite dissolution (pH 3)

## Slide 43
Dolomite dissolution

## Slide 44
In situ AFM observations of wollastonite CaSiO3 dissolution
2 mm
pH 3
Notes: Freshly cleaved {100} wollastonite surfaces show numerous steps parallel to the b-axis (Figure 1a). Initially, dissolution at acidic pH occurs by retreat of pre-existing steps;

## Slide 45
Weathering of minerals
Geology 2016
2012

## Slide 46
Nanoparticle formation
Immediate precipitation on contact of calcite surface with saturated Ca(OH)2
After 20 min

## Slide 47
Notes: 47

## Slide 48
Angelika Kühnle: Tues. 15.08.17 Keynote in Session 08f:
Reactions at the Mineral-Fluid and Mineral-Organic Interfaces: From Molecular Mechanisms to Macroscopic Observations
Notes: 48

## Slide 49
putnisc@uni-muenster.de; christine.putnis@curtin.edu.au
Acknowledgements
Many colleagues have contributed to the research in Münster on dissolution-precipitation reactions:
Encarnación Ruiz-Agudo - Granada, Spain
Helen King – Utrecht, The Netherlands
François Renard - Grenoble, France
Lijun Wang – Wuhan, China
Jörn Hövelmann – GFZ Potsdam, Germany
Andrew Putnis – TIGeR, Curtin University, Perth, Australia
Funding: mostly Marie Curie EU Initial Training Networks;
ARC grant awarded to Julian Gale, Department of Chemistry, Curtin University, Perth, Australia
Notes: 49

## Slide 51
Notes: 51

## Slide 52
No Ca2+ or CO32- pH = 8
{1014} cleavage surface Iceland Spar (ca. 3x4x1 mm)
CaCO3
+
0.01 M HEDP
Hydroxy Ethylene Diphosphonic acid,

## Slide 53
Reaction time: 2.5 hours

## Slide 54
Calcite + 0.5 M NaCl
+ 0.1 M solution NaHCO3

## Slide 55
Reaction time: 40 min

## Slide 56
Mechanism
1. Mineral such as calcite, dolomite, brucite or silicates dissolve congruently in water, releasing ions to solution
2. The mineral-fluid interface becomes increasingly saturated with a new phase (such as, Ca-phosphate or Mg-carbonate or silica), until supersaturation allows precipitation
3. The solution at the interface is then no longer supersaturated and dissolution of the mineral continues until once again supersaturation is reached
4. The cycle is repeated
This is interface-coupled dissolution-precipitation

## Slide 57
In a coupled dissolution-precipitation mechanism the rate-controlling step is dissolution and nucleation is not a problem

## Slide 58
Considerations for the calculation of the boundary fluid layer:
For precipitation to occur, the fluid layer must be supersaturated with respect to the precipitating phase. Therefore we need to know:
1. The solubility of the solid in the fluid phase.
2. The diffusion rate of the solid ions in the fluid phase.
3. The composition of the fluid phase.
4. The saturation index of all possible precipitating phases.
5. Possible epitaxial relationships of the precipitating phase on the substrate.

## Slide 59
Ksp = [Ca2+][HEDP2-] =1.35·10-5 (calculated from Browning and Fogler, Langmuir 1996,11, 4143-4152)
Assuming that precipitation occurs close to the equilibrium and for dilute solutions,
[Ca2+]BL≈ [HEDP2-]/ Ksp ≈ (moles Ca2+)/ VBL
The threshold activities of Ca2+ and HEDP2- are 2.20·10-5 and 1.60·10-4 (calculated from a dissolution rate of 9.17·10-9 mol/s, a time lapse between injections of 90 s and assuming no precipitation of Ca-HEDP phases)
[Ca2+]threshold ≈ (moles Ca2+)/ VFLUID
(moles Ca2+) = [HEDP2-] ·VBL / Ksp= [Ca2+]threshold ·VFREE
VBL = Ksp·[Ca2+]threshold ·VFLUID /[HEDP2-]
VBL = 9.89·10-3 µL
h = 380 nm
VFLUID CELL = 50 µL
VCRYSTAL = 12 µL
h, thickness of the boundary layer
Crystal size = 4x3x1 mm
VFLUID = 38 µL
Calculation of the boundary layer maximum thickness
Notes: 59

## Slide 60
Interface-coupled dissolution-precipitation
Dissolution of even a few monolayers of the parent crystal may result in an interfacial fluid layer which is supersaturated with respect to another phase
(b) This product phase may nucleate on the surface of the parent
a
b
c
d
e
crystal
Notes: 60

## Slide 61
Interface-coupled dissolution-precipitation
(c) The porosity generated depends on both the solid molar volume change and the relative solubilities of parent and product in the fluid
(d-e) A reaction/replacement interface moves through the parent crystal
a
b
c
d
e
crystal
Notes: 61

## Slide 62
A pure crystal of KBr 2 x 2 x 5 mm was placed in a small glass beaker and saturated KCl solution added up to but not covering the surface.
Observations were made using time lapse photography with a camera fitted to a stereoscope microscope.
Experimental set up:
KBr
Saturated KCl solution (0.5ml)
camera
Notes: 62

## Slide 63
Reaction time: 2 hours
Notes: 63

## Slide 64
a
b
SEM image of the porous surface of a KBr crystal after replacement, showing the orientation of pores parallel to cleavage directions:
a) surface of replaced crystal;
b) magnification of (a) from a central area.
Porosity in the new phase
Notes: 64

## Slide 65
Phase Shift Interferometry used to record the solution composition changes at the crystal surface during the replacement process.
Katsuo Tsukamoto and Yoshihiro Nishimura
Tohoku University, Sendai, Japan
Analysis of the fluid phase
Notes: 65

## Slide 66
100µm

## Slide 67
100µm

## Slide 68
Direct in situ observations using
Atomic force microscopy
AFM
Nanoscale observations
Notes: 68